| Scientific Name Dalbergia baronii Trade Name Madagascar rosewood Family Name Leguminosae |  |
| --- | --- |

Common Names 
Madagascar rosewood, Palissandre voamboana

Regions of Distribution 
Africa

Countries of Distribution  [VIEW MAP] 
Madagascar

Common Uses 
Building materials, Carvings, Chairs, Chests, Concealed parts (Furniture), Core Stock, Decorative veneer, Desks, Dining-room furniture, Domestic flooring, Dowell pins, Dowells, Drawer sides, Drum sticks, Excelsior, Factory flooring, Figured veneer, Fine furniture, Floor lamps, Flooring, Furniture , Furniture components, Furniture squares or stock, Hatracks, Interior construction, Interior trim, Joinery, Kitchen cabinets, Living-room suites, Millwork, Moldings, Musical instruments , Office furniture, Organ pipes, Parquet flooring, Piano keys, Pianos , Precision instruments, Shipbuilding, Turnery, Veneer

Environmental Profile

| Status has not been officially assessed |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

Distribution Overview
Madagascar. The species is mainly found in evergreen humid rainforest �at low altitudes, along streams, rivers, in marshy areas and the back of mangrove stands.

Heartwood Color

| Brown |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Yellow |  |  |  |  |  |  |  |  |  |  |  |  |
| Orange |  |  |  |  |  |  |  |  |  |  |  |  |
| Black |  |  |  |  |  |  |  |  |  |  |  |  |
| Gray buff |  |  |  |  |  |  |  |  |  |  |  |  |

Sapwood Color

| White |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Yellow |  |  |  |  |  |  |  |  |  |  |  |  |
| Brown |  |  |  |  |  |  |  |  |  |  |  |  |
| Red |  |  |  |  |  |  |  |  |  |  |  |  |

Grain

| Even |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Straight |  |  |  |  |  |  |  |  |  |  |  |  |

| Straight |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

Texture

| Coarse |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Medium |  |  |  |  |  |  |  |  |  |  |  |  |
| Fine |  |  |  |  |  |  |  |  |  |  |  |  |

Luster

| Low |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

Natural Durability

| Very durable |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Durable |  |  |  |  |  |  |  |  |  |  |  |  |
| Moderately durable |  |  |  |  |  |  |  |  |  |  |  |  |
| Resistant to termites |  |  |  |  |  |  |  |  |  |  |  |  |

The heartwood has very low natural resistance to decay, and should not be used under conditions that promote decay

Drying Defects

| Splitting |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Checking |  |  |  |  |  |  |  |  |  |  |  |  |

Ease of Drying

| Fairly Easy |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Thick Stock Requires Care |  |  |  |  |  |  |  |  |  |  |  |  |
| Rapidly |  |  |  |  |  |  |  |  |  |  |  |  |
| Slowly |  |  |  |  |  |  |  |  |  |  |  |  |
| Little degrade |  |  |  |  |  |  |  |  |  |  |  |  |
| Little degrade if dried properly |  |  |  |  |  |  |  |  |  |  |  |  |
| Easy |  |  |  |  |  |  |  |  |  |  |  |  |

Kiln Drying Rate

| Naturally dries slowly |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Naturally dries quickly |  |  |  |  |  |  |  |  |  |  |  |  |
| Drying rate is fairly rapid to fast |  |  |  |  |  |  |  |  |  |  |  |  |

Tree Size

| Tree height is 20-30 m |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Trunk diameter is 200-250 cm |  |  |  |  |  |  |  |  |  |  |  |  |

Blunting Effect

| High to severe |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

Boring

| Fair to good results |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fairly difficult to very difficult |  |  |  |  |  |  |  |  |  |  |  |  |

Carving

| Very Good to Excellent Results |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fairly Difficult to Very Difficult |  |  |  |  |  |  |  |  |  |  |  |  |

Cutting Resistance

| Easy to saw |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fairly Difficult to Very Difficult to saw |  |  |  |  |  |  |  |  |  |  |  |  |
| Cutting resistance is small |  |  |  |  |  |  |  |  |  |  |  |  |

Gluing

| Fairly Easy to Very Easy |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fair to Good Results |  |  |  |  |  |  |  |  |  |  |  |  |
| Fairly Difficult to Very Difficult |  |  |  |  |  |  |  |  |  |  |  |  |
| Variable gluing properties |  |  |  |  |  |  |  |  |  |  |  |  |

Mortising

| Fair to Good Results |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fairly Difficult to Very Difficult |  |  |  |  |  |  |  |  |  |  |  |  |

Moulding

| Fair to Good Results |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fairly Difficult to Very Difficult |  |  |  |  |  |  |  |  |  |  |  |  |

Movement in Service

| Fair to Good Stability - Medium Movement |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Excellent Stability - Small Movement |  |  |  |  |  |  |  |  |  |  |  |  |
| Shape retention after manufacture is usually good |  |  |  |  |  |  |  |  |  |  |  |  |
| Dimensional stability is generally very good |  |  |  |  |  |  |  |  |  |  |  |  |

Nailing

| Poor to Very Poor Results |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fairly Difficult to Very Difficult |  |  |  |  |  |  |  |  |  |  |  |  |
| Satisfactory nailing properties |  |  |  |  |  |  |  |  |  |  |  |  |
| Pre-boring recommended |  |  |  |  |  |  |  |  |  |  |  |  |

Planing

| Fair to Good Results |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fairly Difficult to Very Difficult |  |  |  |  |  |  |  |  |  |  |  |  |
| Generally easy to use hand tools |  |  |  |  |  |  |  |  |  |  |  |  |
| Easy to use machine tools |  |  |  |  |  |  |  |  |  |  |  |  |

Resistance to Impregnation

| Resistant heartwood |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Resistant sapwood |  |  |  |  |  |  |  |  |  |  |  |  |
| Permeable sapwood |  |  |  |  |  |  |  |  |  |  |  |  |
| Resistant |  |  |  |  |  |  |  |  |  |  |  |  |

Response to Hand Tools

| Easy to Work |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fairly Difficult to Difficult to Work |  |  |  |  |  |  |  |  |  |  |  |  |

Routing & Recessing

| Fair to Good Results |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fairly Difficult to Very Difficult |  |  |  |  |  |  |  |  |  |  |  |  |

Screwing

| Poor to Very Poor Results |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fairly Difficult to Very Difficult |  |  |  |  |  |  |  |  |  |  |  |  |
| Possible if prebored |  |  |  |  |  |  |  |  |  |  |  |  |

Turning

| Fairly Easy to Very Easy |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fair to Good Results |  |  |  |  |  |  |  |  |  |  |  |  |
| Fairly Difficult to Very Difficult |  |  |  |  |  |  |  |  |  |  |  |  |

Veneering Qualities

| Veneers easily |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Suitable for peeling |  |  |  |  |  |  |  |  |  |  |  |  |
| Suitable for slicing |  |  |  |  |  |  |  |  |  |  |  |  |
| Veneers moderately easy |  |  |  |  |  |  |  |  |  |  |  |  |

Steam Bending

| Fair to Good Results |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fairly Easy to Very Easy |  |  |  |  |  |  |  |  |  |  |  |  |

Painting

| Takes oil-based paints with some difficulty |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

Polishing

| Fair to Good Results |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Very Good to Excellent Results |  |  |  |  |  |  |  |  |  |  |  |  |
| Excellent results |  |  |  |  |  |  |  |  |  |  |  |  |

Numerical Data

| Item | Green | Dry | English |
| --- | --- | --- | --- |
| Bending Strength |  | 16961 | psi |
| Maximum Crushing Strength |  | 8663 | psi |
| Stiffness |  | 1742 | 1000 psi |
| Specific Gravity |  | 0.47 |  |
| Item | Green | Dry | Metric |
| Bending Strength |  | 1192 | kg/cm2 |
| Maximum Crushing Strength |  | 609 | kg/cm2 |
| Stiffness |  | 122 | 1000 kg/cm2 |

References
Bolza, E., Keating, W.G.,1972,African Timbers - the Properties, Uses and Characteristics of 700 Species,C.S.I.R.O. Div. of Building Research

Source : http://www.thewoodexplorer.com/maindata/we372.html